## Slide 1
Data driven Dynamic Optimization
of Foundry Sand Testing
Deepak Chowdhary, Director & CEO
MPM Infosoft Pvt. Ltd., India
Developer of ‘SANDMAN (TM)’ Software
30th April 2019

## Slide 2
Virtual Engineering
Smart
Sensors
Cloud
Computing
Internet of Things (IOT)
Data Analytics
Elements of Foundry 4.0
Outcome
Process Optimization by Integrated Digitalization to make better castings, most efficiently, cost-effectively & profitably
Data-Centric
Foundry Transformation

## Slide 3
Virtual Engineering
Cloud Computing
Data Analytics
Process Simulation in Software Environment –Flow & Solidification Simulation; Machine Learning tools
Smart Sensors
Internet of Things
Enables equipment to collect process properties data in digital format – Humidity & Temperature sensors
Enables the real time exchange of data – Molding Line and Mixer SCADA, ERP and Compactability Controller Integration; and online measurements
Advanced Machine Learning Algorithm applied on big databases to Optimize foundry process
Centralized data storage, anywhere accessibility, cloud server based programing and computing application which can also be accessed over the internet
Elements of Industry 4.0

## Slide 4
Globally, all foundries suffer casting rejections.
Some suffer more, some less.
Rejections are repetitive. So, losses are repetitive.
By rule of thumb almost 50% of total foundry rejects are related to sand.
Back-of-the-envelope calculation:
the cost of a
1%
Molding sand Rejection …
…in an entry-level
24,000
ton/annum foundry…
…Is approx. US$
$225,000
per annum

## Slide 5
Blind
Spot
The ‘Why’ of Repetitive Rejections -> Reactive Decision Making
The ‘Blind’ Spot
Process Variability
Foundry Data
Experiential
Legacy
The
Un-Met Need
Predict causality of rejections
Reactive to Proactive Decision making
Shrinking Pool of experts
Non-annotated legacy of events
Un-validated for accuracy, frequency
Un-correlated to rejections
Multiple pockets
Varying Product mix
Varying Sand to Metal ratio
Lack of return sand estimation

## Slide 6
§ To graduate from reactive decision making
by predicting the Highest Influencing sand properties for rejections of the day
§ To move towards ‘dose-by-need’, variable additions of additives.
Prevent overdosing / under-dosing the system sand. Optimizing consumption
§ To move towards dynamic process consistency:
by predicting and then optimizing the optimal target sand properties
§ To control and reduce rejections
By achieving a Dynamically Stable Operational state of the molding process
Motivation for Data Analytics Decision Support
Personal Technical Skills
Experiential Knowledge
Process Database
Data
Profit by Process Optimization
Foundry Data Analytics
Cloud Computing

## Slide 7
Absence of meaningful and authentic data
Different degrees of variability in different sand properties
Challenge in maintaining the optimal range of sand properties
Right Data at right time and at right frequency
Data capturing Frequency of sand properties depending on their variability
Sand Data Correlated to Casting Rejections
ISSUES
REQUIREMENTS
Challenges in Data Analytics based
System optimization
CHALLENGE

## Slide 8: Literature – Foundry Process Optimization & Analytics
Optimization Approach | Researchers / Year | Remark / Summary
Non-linear Optimization Model | D. Chowdhary, et. al., 2018 | Prescriptive model for optimizing sand properties and additives consumption
Artificial Neural Networks and Genetic Algorithms | D. B. Karunakar, et. al., 2007 | Predictive model for mold properties predictions. Genetic model was found to be performing better over Artificial neural network
Response Surface Methodology, and propagation of Error | C. Saikaew, et. al., 2012 | Optimization of molding sand composition for yielding optimal sand properties
Taguchi DOE & Optimization | G. Patil, et. al., 2014 | Process properties are Optimized for minimizing Casting Rejections.
Experimental Design and Bayesian Inference Optimization | H. Khandelwal et. al., 2018 | Relatively new technique applied for Molding composition optimization for Chemically Bonded System
Data Analytics Driven Optimization | S.N. Ramrattan et.al 2016 | Predictive Analytics to Predict Highest Influencing sand properties impacting casting rejections
Optimization by Process Automation | J. Furness et. al. 2018 | Automated Thermal Moisture Analysis, and Automated adjustment of Mixer/Muller energy inputs
No published research was found which determines the optimum sand testing frequency.
GAP

## Slide 9
Present Sand Testing Practice
Approach to Decide Tests & their Frequencies
American Foundry Society (AFS) Standard:
AFS has published the standard for sand measurement for green sand foundries [AFS Mold and Core Test Handbook]
Legacy based Frequency:
Based on the sand plant experience and legacy foundry practice, standard testing frequencies are determined
Time for measurement:
Depending upon the time taken for measurement, e.g., Active Clay and LOI take more time to test, than Compactability.
Resource Availability:
Depending upon the number of staff and equipment available for sand testing.

## Slide 10
BCG Matrix
for testing frequency and resource availability
Present Sand Testing Practice
Testing frequency v/s resource availability
?
Possibility of data inaccuracy

## Slide 11
LIMITATIONS WITH CURRENT SAND TESTING PRACTICE
Testing of Sand without sufficient, authenticated and meaningful data insights on how it impacts the casting outcomes (quality) will have time and cost impact.
Absence of scientific methods that can determine optimal frequency of sand testing based on the causality of the inter-relationship of sand properties to casting rejections.
Static testing Frequency in spite of different variability of sand properties for different periods
Sand Testing Frequency for each component is the same irrespective of variable production planning.
Present Sand Testing Practice
Limitations

## Slide 12
“An analytical solution to predict optimal frequency of sand testing properties in a day/shift based on the cause and effect relationship of rejections with sand properties”
Research Objective
Methodology for Sand Measurement Optimization
Proposed
Sand Testing Frequency Optimized (STFO) Algorithm

## Slide 13: Data Analytics & Cloud Computing for Foundry
SANDMAN, is the world's first (patented) SaaS delivered, Cloud based predictive and prescriptive
analytics software product to enable foundries to optimize their molding sand and as a corollary;
REDUCE CASTING REJECTIONS and OPTIMIZE ADDITIVES CONSUMPTION.
Primary Input
for the algorithm
Machine learning model identifies Highest Influencing Sand Properties (HIP) based on their influence on the casting rejections and suggest the direction of change to reduce the influence
STFO Input – 1

## Slide 14
Predictive Analytics
Predicted rejection, and ‘optimum’ point
Highest influencing properties to tweak
Effect on rejection, if tweaked
Leveraging HIP:
Model Input - Average High Influence Factor (model predicted) for past 15 days of the data available, and scaled to 1 to 10.
Weightage Optimization - Properties with high impact factor on rejections are given more weightage
STFO Input – 1

## Slide 15
ACKNOWLEDGING Variability:
Important input parameter for the algorithm is the variability measure of each sand properties.
Model inherently computes the standard deviation of each properties from the previous three-month data.
The variability is calculated across the shifts and within the shift and scaled to 1 to 10.
Properties with high variability, are given more weightage and therefore need to be tested greater number of times for focused monitoring and control.
Low Variability
Medium Variability
Mean
High Variability
Frequency
STFO Input – 2

## Slide 16
CONSTRAINTs on Time allocation for measurement :
properties | Time for Measurement (min: sec) |  | 
 | Manual | Machine | Total
GCS | 00:16 | 00:32 | 00:48
Compactability | 00:25 | 00:25 | 00:25
Active Clay | 10:05 | 105:00 | 105:00
Wet Tensile Strength | 00:16 | 00:45 | 00:61
LOI | 00:35 | 165:00 | 165:00
Moisture | 00:19 | 30:00 | 30:19
Inert Fines | 00:15 | 90:00 | 90:00
Volatile Matter | 00:35 | 10:00 | 10:00
Permeability | 00:15 | 00:14 | 00:29
Shear Strength | 00:15 | 00:30 | 00:45
GFN/AFS | 15:00 | 15:00 | 30:00
Total Clay | 00:15 | 90:00 | 90:00
Temp of sand | 00:10 | 00:10 | 00:10
Friability Index | 00:40 | 00:30 | 00:70
The total time for measuring each sand properties are split into man-hours and machine-hours.
e.g. For example, during LOI testing the manual time required is only 35 sec, whereas the total time of LOI measurement is 165 min.
Majority of the time is taken by the testing equipment.
During intervening test time, the man/hour available is often utilized for measuring other properties.
The algorithm considers both man and machine time as two separate properties in modelling,
Final optimized solution is being predicted for optimizing both man and machine time available to ensure effective utilization total time.
Time distribution of sand testing practice of a large-scale foundry in India.
STFO Input – 3

## Slide 17
properties Name | Influencing Factor (no.) | Variability (σ) | Measurement Time (min : sec) | Frequency for Sand Measurement (no./shift) | 
 |  |  |  | Present | Optimal
GCS (gm/cm2) | 7.7 | 1.2 | 00:48 | 5 | 5
Compactability (no) | 2.3 | 2.0 | 00:25 | 5 | 5
Active Clay (%) | 1.4 | 5.1 | 105:00 | 1 | 1
Wet Tensile Strength (gm/cm2) | 1.0 | 4.3 | 00:61 | 5 | 5
LOI (%) | 2.6 | 10.0 | 165:00 | 1 | 1
Moisture (%) | 2.6 | 2.1 | 30:19 | 5 | 2
Inert Fines (%) | 10.0 | 5.1 | 90:00 | 1 | 2
Volatile Matter (VM) (%) | 1.7 | 6.8 | 10:00 | 1 | 4
Permeability (no) | 2.6 | 4.8 | 00:29 | 5 | 5
Shear Strength (gm/cm2) | 7.8 | 4.3 | 00:45 | 5 | 5
Friability Index (%) | 4.6 | 1.0 | 00:70 | 5 | 4
Temp. of Sand after mix (°C) | 1.6 | 3.0 | 00:10 | 5 | 5
Case-Study
Optimized frequency solution along with the model input and predicted frequency output for each properties
Inert Fines
1 → 2
Moisture
5 → 2
GCS
5 → 5
VM
1 → 4
LOI
1 → 1
Influence: Maximum Variability: Medium Time: High
Influence: Low Variability: Low Time: Medium
Influence: High Variability: Low Time: Low
Influence: Low Variability: High Time: Medium
Influence: Low Variability: Maximum Time: High
Notes: Maximum frequency : Maximum frequency will be restricted to the average maximum frequency for any parameter in historical data.

## Slide 18
Time distribution based on foundries present testing frequency
Time distribution based on foundries optimized testing frequency
Chart: % Time Distribution of Shift 1
| Active Clay (%) | Compactability (no) | GCS (Kg/cm2) | Temp. of Sand after mix. (C) | Friability Index (%) | Shear Strength (Kg/cm2) | Permeability (no) | Volatile Matter (%) | Inert Fines (%) | Moisture (%) | LOI (%) | Wet Tensile Strength (gm/cm2)
 | 0.396 | 0.085 | 0.056 | 0.035 | 0.113 | 0.053 | 0.053 | 0.09 | 0.019 | 0.02 | 0.023 | 0.056
Chart: % Time Distribution of Shift 1
| Active Clay (%) | Compactability (no) | GCS (Kg/cm2) | Temp. of Sand after mix. (C) | Friability Index (%) | Shear Strength (Kg/cm2) | Permeability (no) | Volatile Matter (%) | Inert Fines (%) | Moisture (%) | LOI (%) | Wet Tensile Strength (gm/cm2)
 | 0.396 | 0.088 | 0.056 | 0.035 | 0.14 | 0.053 | 0.053 | 0.023 | 0.01 | 0.067 | 0.023 | 0.056
Case-Study

## Slide 19
properties Name | Absolute Variability | 
 | Actual | Simulated
GCS (kg/cm2) | 0.09 | 0.09
Compactability (no) | 1.37 | 1.37
Active Clay (%) | 0.49 | 0.49
Wet Tensile Strength (gm/cm2) | 2.16 | 2.16
LOI (%) | 0.31 | 0.31
Moisture (%) | 0.08 | 0.08
Inert Fines (%) | 0.24 | 0.17
Volatile Matter (%) | 0.16 | 0.08
Permeability (no) | 4.47 | 4.47
Shear Strength (kg/cm2) | 0.04 | 0.04
Friability Index (%) | 0.52 | 0.51
Temp. of Sand after mix (°C) | 1.17 | 1.17
Steps for generating simulated data-set –
STFO Model Validation
A validation experimentation to understand the value proposition
– Compared sand properties variability before and after optimization.
Variance of Previous three-month prepared sand data calculated in its original space and for simulated data-set.
The standard deviation of the properties in the Simulated data is found to be reduced with optimized sand testing frequency
Conditional Situation
Optimal frequency = Actual frequency
Optimal frequency < Actual frequency
Optimal frequency > Actual frequency
Data Preparation Method
The data remained unchanged – No Change
The starting data in each-shift is considered and ignored remaining .
The data is imputed by shift-wise mean of that properties

## Slide 20
Enhancement in STFO
Group Wise Testing Frequency
Casting based Sand Additive Requirement
Automated Grouping (e.g. S:M ratio) Algorithm
Group-1
Group -’n’
Group Wise Modelling
Optimal Testing Frequency for each Group
  STFO Inputs –
  Group-wise Sand properties Variability
  Group-wise Influencing Factor

## Slide 21
STFO driven solution helps foundry to generate more meaningful data and will have better sand optimization with controlled process consistency.
Conclusion
Making Sand Testing Dynamic Rather than Static
Direct Utilities of Optimized Sand Testing Frequency
STFO generates meaningful time-series data for algorithms like SANDMAN® that are designed for sand system optimization by Machine learning and AI methodology
Accurate predictions and prescriptions by data analytics, keeps the system sand optimised consistently, sustainably and scalably.
STFO Increases the frequency of tests of the highest influencing properties which will help foundry in closely monitoring the same.
STFO Reduces the frequency of the lowest influencing properties or properties with less variability in order to optimize utilization of man / machine time
STFO can help in-time decision making by the QC department in controlling influencing sand properties and as a corollary, help improve casting quality.

## Slide 22
MPM INFOSOFT and the SANDMAN Team wish to thank “AFS and Distinguished Leaders of the Foundry Industry” for the invaluable opportunity to address and present STFO concept at the “Cast Expo 2019”.