## Slide 1: Use of Green Sand Additives as Essential Contaminants
Mr. Deepak Chowdhary
Founder & Managing Director
MPM Pvt. Ltd., India
Manufacturer of Lustrous Carbonaceous Additives

## Slide 2
A Perspective on Additive Control in Molding Sand
The straight forward objective of this simple mix is to prevent Metal-Mold reaction
“However, this simple mix of these 4 basic additives becomes complex when exposed to the dynamics of the circulating system sand of a foundry”
Raw Sand
The most refractory material in the sand mold
Bentonite
The most cost effective high temperature, sustainable binder for the raw sand
Ancillary Additives
Water
Coal Dust
Essential to activate the gelling/binding properties of Bentonite
Most effective low cost Lustrous Carbon de-oxidant to help prevent sand-metal reaction
Dextrin, Wood Flour, etc., used based on the specific requirement
Principal additives used for preparing Sand Molding

## Slide 3
Increase in Total Surface Area (TSA) of the Total Sand
Increase in Moisture Demand/Temper Water
Uneven Compaction
of the Mold
Lowering the Fusion Point of the Molding Sand/Reduced
Sand Refractoriness
Increased Sand Sticking
Reduced Permeability
Lower Flowability of Sand
The Big ?
The Need for the Perspective on Additive Control
MAJOR EFFECT OF MORE THAN NECESSARY USE OF ADDITIVES
What is the Optimum Additive Consumption?

## Slide 4
Varying Product Mix
Varying Core sand Influx
Varying Total Surface Area of Sand
Inter-relationship Between Sand Properties
Return Sand
Cycles and
Resultant Layers in
the Return Sand
hopper
Multivariate Cause and Effect Between Sand Parameters and Additives
Impact on Casting Defects
Reactive Decision on Additions
Return Sand Measurements – the ARBITRAGE GAP
Return Sand Hopper
Challenge of Using Optimum Level of Additives

## Slide 5
Effect of Interrelationship Between Sand Properties
*PARAMETERS | INCREASE | MOISTURE | COMPACTABILITY | ACTIVE CLAY | GCS4. Slide 4 | PERMEABILITY | INERT FINES | LOI | WTS | SHEAR STRENGTH | SHATTER INDEX | GFN | SPECIMEN WEIGHT | FRIABILTY INDEX
TEMPER MOISTURE | ↑ |  | ↑ | X | ↑ | X | X | X | ↑ | ↑ | ↑ | X | ↓ | ↓
ACTIVE CLAY | ↑ | X | ↑ |  | ↑ | ↓ | X | X | ↑ | ↑ | ↑ | ↓ | X | ↑
The change in any property can impact several sand properties simultaneously
Direction | 
Increase | 
Decrease | 
No Change | 
Likely | 
Legend
*Table is a partial list of sand parameters

## Slide 6
Active Clay
pH value
WTS
GSS
Moisture
Friability
Inert Fines
GCS
Permeability
Specimen Weight
Shatter Index
Compactability
Control
Sand Parameters
Impact of Additives & Interrelationship Between Sand Properties
ADDITIVES | Increase | GCS | Shear Strength | Shatter Index | Moisture % | Wet Tensile Strength | PH Value | Permeability | Specimen Weight | Compactability | Friability | L O I | V M | Active Clay | Inert Fines | AFS No.
SODIUM BASE BENTONITE | ↑ | ↑ | ↑ | ↑ | O | ↑ | ↑ | ↓ | ↑ | ↑ | O | X | X | ↑ | O | X
LUSTROUS CARBON ADDITIVE | ↑ | ↓ | ↓ | ↓ | X | ↓ | ↓ | ↑ | ↓ | ↓ | ↑ | ↑ | ↑ | X | X | O
FRESH SILICA SAND - HIGH GFN NO. | ↑ | O | O | O | O | O | X | ↓ | ↑ | O | O | X | X | X | X | ↑
Decrease in Bentonite

## Slide 7
Chart: Total Surface Area relationship to Core Sand Influx Impact on Varying Additive demand
| PT BLOCK | ESCORT PT block | MDI Block | LCCR Block | Escort FT block | M-Star
CORE WEIGHT | 78.25 | 78.25 | 131.24 | 131.24 | 99.66 | 97.9
SURFACE AREA | 93.92 | 104.02 | 90.2 | 85.88 | 80.42 | 92.12
AFS NUMBER | 47.54 | 52.68 | 45.67 | 43.42 | 40.62 | 46.6
“By far, the most important and overlooked impactor of variation in green sand preparation, is the Total Surface Area (TSA) of the molding sand”
TSA – Total Surface Area of Molding Sand
Reasoning: each pattern return sand will form a layer as it re-circulates into a storage hopper
The TSA of sand layer for the next molding batch mix can only be estimated
The motivation is to examine the variability of the TSA of the sand before it goes into the mixer
The variability will decide how much make-up additives are required to achieve target properties
Core Sand Infiltration at varying percentage affects molding sand GFN; thereby TSA

## Slide 8
Impact on flowability of the system sand:
All additives, while imparting essential properties to the molding sand, essentially also serve to reduce/increase its flowability
Flowability is a crucial KPI of the molding sand as it enables/inhibits the delivery of the sand to all edges, corners and contours of the cavity
Lowers the fusion point of the molding sand and reduces sand refractoriness:
None of the additives added to the molding sand have the fusion point of the silica sand (1650-1750 °C)
Additives like Bentonite lead to lowering the sintering point of the sand
Increased levels of active clay are empirically associated with increased sand-sticking and ‘burn-on’
Impact of Increased/Decreased Additive demand
”Most importantly, overdosing additives increases inert fines build up”

## Slide 9
Outlook of Additives on Inert fines build up
Inert Fines ~ 3-4 %
Helps in Smoothening out the free moisture
Helps in development of the adjoining active bentonite particles
Inert Fines > 3-4 %
Increased obliteration, friability and explosive penetration
Empirical Relationship
Inefficient, poor-quality or of additives
Higher additions of Bentonite and Coal Dusts (OVERDOSING)
Increased burn outs and buildup of Inert Fines
The dust collector extraction will not be limited to the dead fines due to burn outs of the additives but also the fines of active bentonite and un-burnt carbonaceous dusts.
These are never fully refluxed back into the circulating sand due to reasons of their GFN which can upset the total surface area balance further compounded by handling issues like air pollution, from the POC (Point of Collection) to the POU (Point of Use).

## Slide 10
Bentonite Impact on Moisture Demand and Inert Fines
The increase/decrease in the surface area of the system sand is the corresponding increase/decrease in the moisture demand and temper water point.
Courtesy : SANDMAN

## Slide 11
Beyond optimum use of Bentonite more often than not, leads to sand sticking and sand fusion on the casting surface (example: lower sintering point of the Bentonite, increase in Inert Fines and Moisture demand)
Chart: Bentonite v/s Casting Finish
| 01.06.17 | 02.06.17 | 03.06.17 | 5.06.17 | 6.06.17 | 7.06.17 | 8.06.17 | 9.06.17 | 10.06.17 | 12.06.17 | 13.06.17 | 14.06.17 | 15.06.17 | 16.06.17 | 17.06.17 | 19.06.17 | 20.06.17 | 21.06.17 | 22.06.17 | 23.06.17 | 24.06.17 | 25.06.17 | 27.06.17 | 28.06.17 | 29.06.17 | 30.06.17 | 3.07.17 | 4.07.17 | 5.07.17 | 6.07.17 | 7.07.17 | 8.07.17 | 10.07.17 | 11.07.17 | 12.07.17 | 13.07.17 | 14.07.17 | 15.07.17 | 17.07.17 | 18.07.17 | 19.07.17
Bentonite (kg/mould) | 14.9469 | 13.7084 | 13.3676 | 14.0819 | 14.5624 | 14.5463 | 14.2421 | 13.8595 | 14.8287 | 16.5781 | 14.3686 | 14.7982 | 14.037 | 14.6129 | 14.2778 | 14.4597 | 13.3508 | 12.5865 | 13.1266 | 13.181 | 13.1255 | 13.7639 | 13.3333 | 12.3693 | 12.8337 | 12.9934 | 13.1391 | 12.625 | 13.2521 | 13.2386 | 12.6894 | 13.0062 | 13.1901 | 12.389 | 12.7361 | 12.9709 | 13.1837 | 12.7105 | 12.3431 | 12.4388 | 12.5929
Surface Finish Index (no.) | 6.2105 | 5.6154 | 5.6786 | 5.2857 | 5.4444 | 4.7391 | 4.5769 | 4.7391 | 4 | 5.125 | 5 | 4.9259 | 5.1538 | 5 | 4.7692 | 4.6818 | 4.5833 | 4.8148 | 5.1071 | 5.32 | 5.2963 | 5.4643 | 5.9643 | 6.1852 | 6.4444 | 6.2609 | 6.2917 | 6.8571 | 6.8947 | 7 | 7.56 | 7.6818 | 8.2174 | 7.8571 | 7.7692 | 8 | 7.8571 | 7.7391 | 7.6 | 7.7692 | 7.8571
Impact of Bentonite on Casting Surface Finish
Courtesy : SANDMAN

## Slide 12
Higher additions of additives, clay and starch leads to reduced permeability with possible related risk of blow hole defects.
Impact of Bentonite on Permeability
Courtesy : SANDMAN

## Slide 13
What is the optimum additive consumption?
Data Analytics & Decision Support
Domain & legacy based Human Expertise
Additives Source & Quality based on Key Performance Properties
“The use of data science and analytics is the scientific answer to predict the precise optimal points for each sand property, based on the inter-relationship between sand parameters and also co-related to casting defects (scrap)”
Optimal

## Slide 14
Monitor the TSA for variability of additive demand. This is the pulse for all additive demand.
Avoid over/under dosing of Active Clay/Lustrous Carbon/Water etc., by always taking into account the inter-relationship between sand properties before reacting with dosage or source or quality change
Always choose additives based on their KPI :
  Consider the purpose the KPI has to serve and then its cost
Establish Additive KPI beyond conventional tests. There is always something more that you should know. Seek expert help, read widely and go deep into understanding the additives (example: bentonite or coal dust).
How should optimum additive consumption be monitored?

## Slide 15
Adds significant and competitive value in terms of:
Cost saving when added in variable and optimal quantities, co-related to varying casting product mix, source and quality.
Re-claiming repetitive lost profits by improving process consistency thereby
  achieving reduced, related casting rejections
  optimized additive consumption.
Improving Casting productivity & quality of surface finish
Maintaining a dynamically sustainable, stable and scalable balance in sand control process consistency
Summary : Benefits of Using Additives with the perspective of being essential contaminants

## Slide 16
MPM INFOSOFT and the SANDMAN Team wish to thank
World Foundry Organisation, Polish Foundrymen’s Association, 73rd WFC and the
Distinguished Leaders of the Foundry Industry
for the invaluable opportunity to address and present ‘Use of Green Sand Additives as Essential Contaminants’.